# Painting of metal products

## Why products are painted?

Painting of metal products is used to give the products surface properties that it doesn’t have naturally. Without painting metal products start to rust and erode and in case of wood products surfaces are easier to clean when they have a lacquer layer on them. So, the surface durability of the products is improved with painting. In addition, the surface color can be freely chosen, the shininess of the surface can be adjusted, and the surface structure can be adjusted. Painting can also be used for insulation such as fire insulation, humidity insulation and hygienic insulation. Painting increases the cost of manufacturing but it’s aim is to increase the life cycle of the product, lower the cleaning costs for the surfaces and to give the product a good-looking finish. Generally painting can be divided into two distinct categories. Painting for corrosion protection and painting for looks but often the needs overlap and both are needed. Corrosion protected paint coat is typically multi layered wet coat that is painted with high-pressure spray-painting machinery. When demanding good looking finish, the shininess of the surface, evenness of the paint coat, evenness of the color and wear resistance of the coating are some common demands. Common painting methods for good-looking finish are powder coating or wet painting.

## Chemical pretreatment of products

Chemical pretreatment is used to process the surface of products so that the surface can be coated with paint or other coating methods without problems. Chemical pretreatment is used for products that are manufactured from steel, zinc coated steel or from aluminum.

|  |  |  |
| --- | --- | --- |
| Impurity | Source of impurity | How to remove |
| Safety oil and grease | Added during manufacturing to prevent rusting | Mineral oils removable by water or solvent based washing procedures. Vegetable and animal greases hard to remove |
| Salts | Transportation or from human hand sweat | Removable by water-based washing procedures |
| Carbon dust and soot | Cold rolling | Removable by alkali or solvent based washing procedures |
| Cutting fluid | Sawing, milling, etc | Removable by water-based washing procedures |
| Pulling lubes and soaps | Manufacturing of wire and tube products | Removable by water-based washing procedures |
| Metal chips | Metalworking processes | Mechanical washing |
| Rust and surface rust | Storing in humid conditions, “old” material | Can’t be removed by washing. Acid pickling required or mechanical processing. Surface rust removable by chemical procedures |

Table 1: Impurities on metal surfaces

Results of chemical pretreatment are affected by four different factors. Them being used chemical, temperature, time, and mechanical movement. These four factors make up a cleaner’s circle, often known as a Sinner’s circle.

Kuva, joka sisältää kohteen ympyrä, keltainen, symboli, viiva

Kuvaus luotu automaattisesti

Figure 1: Sinner’s circle

Breaking down the Sinner’s circle:

1. Chemical: Chemicals used in cleaning need to be capable of removing the desired impurity from the material. It’s also important since other three factors can’t be increased indefinitely. The concentration of the chemical can be increased to increase its effectiveness and it needs to be kept clean. Chemicals lose their effectiveness when used for cleaning and the removed impurities need to be removed from chemical if it is to be reused. Often that isn’t financially feasible, and the cleaning chemical can be said the be one time use only.
2. Mechanical movement: Mechanical movement improves the results of washing and often it is mandatory for a good result. Movement can be produced by a few different methods. In spray washing processes the movement is produced by the spraying itself. In immersion washing the movement can be produced by pumping, where the solution bath is mixed by pumping the solution out and back into the bath. Alternative method is to use a mixer that uses blades to mix the solution. Ultrasonic sound can be used to drastically increase the results of the washing. Ultrasonic can also remove impurities that can’t be removed normally by washing procedures. Blowing air into solution is a simple way to create movement that improves results. Downside being it creates fumes which means that it isn’t preferrable when using chemicals that have solvents. It creates fumes even when the solution is fully water based and lowers the temperature of the solution bath which decreases the results of wash. It’s better used for rinsing the parts than in active cleaning. Used air in also needs to clean and free of oils. Movement can also be simply introduced by moving the work piece in solution. Movement is also important in rinsing where the remaining solution is removed from work piece.
3. Time: Time is an important part for the results of washing. By increasing the time work piece spends in solution bath the better results can be expected. But too long time can damage washed work piece and can create deposits that are hard to remove. Long time will also increase the cost of pretreatment.
4. Temperature: Increased temperature improves washing results. Different chemicals have different operating temperatures so temperatures should match the used chemicals. Too high temperature increases water evaporation, chemical fumes, and energy costs.

## Choosing the correct pretreatment method